## Flat Fiber Cement Sheets - 20 mm

Certified ISO 9001:2004, ISO 14001:2004, and OHSAS 18001:2007.

Fiber cement sheets are Type A, Grade 1, according to standard ASTM C 1186-07 and Type A, Category 2, according to standard INTE/ISO 8336:2007.

### Technical Specifications

| Description | Min. Value | Max. Value |
| --- | --- | --- |
| Resistant to bending (dry) (N/mm2) | 9.0 |  |
| Elastic module (dry) (kN/mm2) | 2.5 | 4.0 |
| Density (kg/dm3) | 1.0 | 1.2 |
| Humidity (%) |  | 10.0 |
| Total absorption (%) |  | 40 |
| Surface absorption (%) |  | 25 |
| Humidity movement (mm/m) |  | 1.3 |
| Total contraction (mm/m) |  | 4.0 |
| Water absorption (Karsten) (ml/24h) exposed face |  | 1.5 |
| Smoke developed | 0 |  |
| Flame propagation | 0 |  |

### General Information

Fat fiber cement sheets are a product used in installing mezzanines on a metal or wood structure. They are capable of safely standing up to the forces generated by temporary or permanent loads. They may be used to install any type of floor and are available in a natural gray color.

### Advantages

### Product Components

- Conventional tools may be used to:

  - cut and sand them;

  - drill holes in them; and

  - secure them with nails and screws.

- They provide insulation against noise and heat.

- They will take any type of finish.

- They are humidity, mold, and fire resistant.

Portland Cement, calcium carbonate, cellulose fibers, and other lesser aggregates. Flat fiber cement sheets meet requirements for resistance, safety and durability required in constructing buildings with the strictest environmental regulations. The surface of the flat fiber cement sheets is treated with an impregnating emulsion that makes them repel water and maintain their permeability to water vapor.

### Manufacturing and Quality Control

### Nominal Dimensions

| Dimension | Measurement (mm) | Tolerance (mm) |
| --- | --- | --- |
| Thickness | 20.0 | ± 0.6 |
| Width | 1,219 | ± 2 |
| Length | 2,438 | ± 2 |
| Diagonal | 2,726 | ± 2 |

### Other Characteristics

### Certifications

| Weight (kg/unit) | 67.88 |
| --- | --- |
| Covering per Unit (m2) | 2.97 |

Consultas sobre instalación y garantías en www.plycem.com o al teléfono 2575-4300.
Propiedad de The Plycem Company. Únicamente para uso informativo del cliente.
Edition: 02 - Fecha de Emisión: Mayo 2014
Página 1 de 1