## Flat Fiber Cement Sheets - 8 mm

Certified ISO 9001:2004, ISO 14001:2004, and OHSAS 18001:2007.

According to standard ASTM C 1186-08 (2012) and are certified as category A, Class 2, and Category B, Class 2, according to standard INTE/ISO 8336:2011.

### Technical Specifications

| Description | Min. Value | Max. Value |
| --- | --- | --- |
| Resistant to bending (in equilibrium) (N/mm2) (ISO 8336/ASTM C 1186) | 7.0 |  |
| Elastic bending module (in equilibrium) (kN/mm2) ISO 8336/ASTM C 1186) | 2.5 | 4.0 |
| Density (kg/dm3) (ISO 8336) | 1.10 | 1.20 |
| Humidity (%) (proprietary procedure) | 0.0 | 8.0 |
| Total absorption (%) (ASTM 1186) |  | 40 |
| Cobb surface absorption (%) (proprietary procedure) |  | 25 |
| Humidity movement (%) (ISO 8336/ASTM C 1186) |  | 0.13 |
| Total contraction (mm/m) (proprietary procedure) |  | 3.0 |
| Water absorption (Karsten) (ml/24h) exposed face (proprietary procedure) |  | 3.0 |
| Smoke developed (ASTM E - 84) | 0 |  |
| Flame propagation (ASTM E - 84) | 0 |  |

### Nominal Dimensions

### General Information

Flat fiber cement sheets are a product designed to cover the interior and exterior with a monolithic finish (hidden joints). They are resistant to the weather, insects, heats, and humidity. They may be installed on metal or wood structures. They are a high-performance solution for the outdoors and when you are looking for maximum durability, resistance and construction feasibility.

### Advantages

### Product Components

- They may be used on high-traffic walls.

- They are impact resistant.

- Conventional tools may be used to:

  - cut and sand them;

  - drill holes in them; and

  - secure them with nails and screws.

- They provide insulation against noise and heat.

- They will take any type of finish.

- They are humidity, mold, and fire resistant.

Portland Cement, calcium carbonate, cellulose fibers, and other lesser aggregates. Flat fiber cement sheets meet requirements for resistance, safety and durability with the  strictest environmental regulations. The material is able to repel rainwater and maintains its permeability to water vapor.

### Manufacturing and Quality Control

| Dimension | Measurement (mm) |  | Tolerance (mm) |
| --- | --- | --- | --- |
| Thickness | 8 |  | ± 0.6 |
| Useful width | 1,219 |  | ± 2.0 |
| Length | 2,438 | 3,048 | ± 2.0 |
| Diagonal | 2,726 | 3,283 | ± 2.0 |

|  | Sheet Length |  |
| --- | --- | --- |
| Characteristics | 2,438 mm | 3,048 mm |
| Weight - sheets (kg/unit) | 28.78 | 35.98 |
| Useful covering (m2) | 2.97 | 3.72 |

2

### Certifications

Consultas sobre instalación y garantías en www.plycem.com o al teléfono 2575-4300.
Propiedad de The Plycem Company. Únicamente para uso informativo del cliente.
Edition: 01 - Fecha de Emisión: Septiembre 2016
Página 1 de 1