## Tongue and Groove Siding - Hidden Joints

Certified ISO 9001:2004, ISO 14001:2004, and OHSAS 18001:2007.

The siding sheets are Type A, Grade 1, according to standard ASTM C 1186-07 and Type A, Category 2, according to standard INTE/ISO 8336:2007.

### Technical Specifications

| Description | Min. Value | Max. Value |
| --- | --- | --- |
| Resistant to bending (dry) (N/mm2) | 9.0 |  |
| Elastic module (dry) (kN/mm2) | 2.5 | 4.0 |
| Density (kg/dm3) | 1.0 | 1.2 |
| Humidity (%) |  | 10.0 |
| Total absorption (%) |  | 40 |
| Surface absorption (%) |  | 25 |
| Humidity movement (mm/m) |  | 1.3 |
| Total contraction (mm/m) |  | 4.0 |
| Water absorption (Karsten) (ml/24h) exposed face |  | 1.5 |
| Smoke developed | 0 |  |
| Flame propagation | 0 |  |

### Nominal Dimensions

| Dimension | Measurement (mm) | Tolerance (mm) |
| --- | --- | --- |
| Thickness | 14.0 | ± 0.6 |
| Useful width | 240 | ± 2 |
| Length | 2,438 | ± 2 |
| Diagonal | 2,450 | ± 2 |

| Siding weight 24 cm (kg/unit) | 9.35 |
| --- | --- |
| Covering per Package (m2) | 2.92 |

### General Information

Código y nombre comercial: 974315 SIDING MH CLAS 14mm 240X2438mm F/OCULTA

Description: Tongue and groove siding sheets are used in exterior and interior walls as an architectural element in residences and institutional, industrial, and commercial buildings. They use a hidden joint system.

### Advantages

### Product Components

- Hidden joints

- Screws do not stand out in the siding

- Clean finishes

- Easy installation

- May be installed after they are painted

- Conventional tools may be used to:

  - cut and sand them;

  - drill holes in them; and

  - secure them with nails and screws.

- They provide insulation against noise and heat.

- They are humidity, mold, and fire resistant.

Portland Cement, calcium carbonate, cellulose fibers, and other lesser aggregates. Flat fiber cement sheets meet requirements for resistance, safety and durability required in constructing buildings with the strictest environmental regulations. The surface of the sheets is treated with an impregnating emulsion that makes them repel water and maintain their permeability to water vapor. The graphite siding has iron oxide as an aggregate to give it an integral dark gray color.

### Manufacturing and Quality Control

### Certifications

### Other Characteristics

Consultas sobre instalación y garantías en www.plycem.com o al teléfono 2575-4300.
Propiedad de The Plycem Company. Únicamente para uso informativo del cliente.
Edition: 02 - Fecha de Emisión: Mayo 2014
Página 1 de 1